R606.4 Allowable stresses Allowable compressive stresses in masonry shall not exceed the values prescribed in Table R606.4. Concrete masonry units shall be hollow or solid unit masonry in accordance with ASTM C 90 and shall have a minimum net area compressive strength of 1900 psi in compliance with ASTM C 90. Mortar shall comply with Section R607.1. In determining the stresses in masonry, the effects of all loads and conditions of loading and the influence of all forces affecting the design and strength of the several parts shall be taken into account.

(Remaining text unchanged)